Agreement that establishes the goods whose import and export is subject to regulation by the Ministry of Energy.

Goods classified under HS code below are subject to permit requirement C1 (Import permit for hydrocarbons and petroleum products).

***Note: This list shows the goods up to 6 digits, the C1 permit also applies to the rest of the subheadings of each HS code listed.***

|  |  |  |
| --- | --- | --- |
| **HS Code** | **Description** | **Annotation** |
|  | | |
| **2710.19** | **Other:** | none |

**Lubricating oils or lubricating preparations based on mineral oils** derived from petroleum

mineral oils derived from petroleum, with additives (finished lubricating oils).

|  |  |  |  |
| --- | --- | --- | --- |
| **PARAMETERS** | **UNIT OF MEASUREMENT** | **METHOD** | **SPECIFICATIONS** |
| **Appearance** | Not applicable | Visual | Viscous liquid |
| **Specific weight 20/4 °C** | Not applicable | ASTM D1298 ASTM D4052 | 0.80 - 0.94 |
| **Kinematic viscosity at 40 °C** | mm2 /s (cSt) | ASTM D445 | 2.5 minimum |
| **Viscosity index** | Not applicable | ASTM D2270 | 80 minimum |
| **Flash point** | °C | ASTM D93  ASTM D92 | 98 minimum |
| **Temperature of run-off** | °C | ASTM D97  ASTM D5950 | -9 maximum |
| **ASTM Color** | Not applicable | ASTM D1500 | 6 maximum |
| **Type of base oil** | Not applicable | Not applicable | Mineral |
| **Type of additives** | Not applicable | Not applicable | Inform |

* In case of reporting a different method for the determinations of the specifications established in the parameters, the reported value must be within the specified intervals described above.
* The type of mineral oil used must be specified (Paraffinic, Naphthenic or a mixture).
* In the case of the property type of additives, the additives contained in the finished lubricating oil must be reported. finished lubricating oil contains.

**Lubricating greases.**

|  |  |  |  |
| --- | --- | --- | --- |
| **PARAMETERS** | **UNIT OF MEASUREMENT** | **METHOD** | **SPECIFICATIONS** |
| **Appearance** | Not applicable | Visual | Solid or semi-solid |
| **NLGI Grade** | Not applicable | ASTM D217 | 000-6 |
| **Drip point** | °C | ASTM D2265 | 110 minimum |
| **Density at 15 °C** | g/cm3 | ASTM D70 | 0.86 - 0.94 |
| **Temperature of run-off** | °C | ASTM D97 | -12 maximum |
| **Temperature flash point** | °C | ASTM D92 | 150 minimum |
| **Type of base oil** | Not applicable | Not applicable | Inform |
| **Type of soap or thickener** | Not applicable | Not applicable | Inform |

* In case of reporting a different method for the determinations of the specifications established in the parameters, the reported value must be within the specified intervals described above.
* The type of base oil should be reported.
* The type of thickening soap contained in the lubricating grease should be reported.